SGG Technical Statement - Triple Glazing & Thermal Stress

The thermal build up within the cavity of the triple glazed units in conjunction with low emmisivity coatings means that the centre pane is subjected to higher stresses than those experienced by double glazed units.  This build up means that there is a very high probability that the centre pane may become thermal unstable.

Factors such as blinds, overhangs adjacent to the glazing as well as heating systems will also increase the above potential for thermal stress.

Saint Gobain has to date not released a technical sheet to my knowledge with reference to thermal stress within triple glazed units.  With this in mind we would strongly recommend that the centre pane of a triple glazed unit is thermal toughened.

The software available to calculate the above is only available for hermetically sealed double glazed units.

I am sure with increase demand for triple glazing in the market place further programs will be developed.

We will keep you informed of any further developments.

Richard Hickson

Technical Specification Manager

Saint-Gobain Glass UK

M: 07710 358712

Saint-Gobain Glass website